Magnetic horn for a neutrinos factory

Thermal and mechanical issues

1.Horn prototype at Cern – features

During 2002, a magnetic horn prototype was designed and manufactured at Cern. This horn was designed to be able to withstand to high constraints coming from an integrated target : mechanical stress, heat load, neutrons irradiation. These heavy constraints are concentrated in a small area : the waist of horn’s inner conductor.

Considering the unknown material behavior after a high neutrons flux, the first Cern’s mechanical calculations bring this position : Horn’s mechanical strength is critical (fatigue trouble).

2.Thermal issues

According calculations performed by LAL, heat transfer in the horn is close to be critical.

Surface heat flux is near 500 kW/m2 (usual values are below 80 kW/m2)!

For the horn prototype, heat transfer is done with 2 kind of cooling systems :

- sprinklers producing a water curtain

- internal jacket giving an annular channel

A different approach is proposed by LAL :

To reduce thickness (of inner conductor’s waist) leads to a heat load reducing. Thus, the cooling system can be changed for a unsophisticated one (with a good mechanical behavior keeping).

A first analytical calculation confirms this position. Complete numerical calculations will be performed later.

To be able to performed these numerical calculations with right data, a ‘thermal bench’ will be manufactured and used at LAL. Thermal behavior and heat transfer coefficients will be checked for the critical area of horn (for inner conductors as designed by LAL and Cern).

3.Material and mechanical issues

After a 6 weeks working, the high fast neutrons flux (~ 1022/cm2) leads to a new material behavior : Aluminum alloy becomes brittle and bubbles arise and grow in the material. These bubbles are potential fatigue cracks, which would probably reduce the fatigue strength.

Unfortunately, fatigue behavior of irradiated aluminum is unknown, and fatigue tests of a such irradiated material is very expensive (~300 k€). Thus, it will be done only fatigue tests of non-irradiated to show an expected fatigue limit around 1010 cycles.

A first analytical calculation confirms the horn’s fatigue strength, and indicate an infinite lifetime. However, considering the material alteration after 6 weeks working, lifetime is reasonably set to 6 weeks.

Complete numerical calculations will be performed later :

- FEM transient analysis, to show inner conductor behavior during start up (and ‘continuous’ behavior in case of using a low repetition rate power supply [~1Hz])

- FEM harmonic state analysis (at 50 Hz), to show inner conductor behavior after start up

4.Summary

According to first calculations, mechanical strength and heat removal (from inner conductor) is achieved for a inner conductor with :

- a double skin (Cern’s prototype)

- a single heat exchange surface (LAL proposal)

However, studies and tests have to be done to optimize the horn’s inner conductor following the LAL’s design, which brings :

- better transparency

- lower manufacturing cost

- well known dynamical behavior (easy FEM modeling)